OPPONENT'S  REVIEW

of PhD. dissertation thesis

Author: 	Ing. Eva Hnátková

Title: 		Influence of binder composition on powder injection moulding process

Opponent:	prof. Ing. Pavol Alexy, PhD.

The submitted thesis are focused on investigation of main components influence on processing behaviour of composites for PIM technology. Rheological, mechanical and thermal properties were studied. The work has a range of 100 pages of text, tables and images, including 87 references with cited of four own papers related to discussed results. The literature sources are well chosen and appropriately used. The work is divided into separate chapters, written in clear manner.

Results of the thesis are based on own large experimental work and calculations. Discussion of obtained results is done in deep details with confrontation to other authors. Based on obtained results influence of all components on basic properties of PIM blends is very well discussed.

The dissertation thesis is of a very high level of quality (in its content as well as the formal processing). I have two questions:

- Non-Newtonian index n was calculated based on linear or polynomial regression. Linear model represents Ostwald de Wael equation, which appears insufficient for precise description of flow curve. Probably it is mainly due to fact that flow curves cover not only transition region but partly also the second Newtonian plateau. Why author use for description of such flow curves polynomial approximation of n instead application of other models like for example Sisko – Elis, Cross, Carreau etc.?

- Debinding process based on dissolving of PEG leads in case of higher temperatures to destroying of some parts of moulded specimen. On the other hand, lower temperatures prolong extraction process. It appears that the suitable solution should be the process with programmed temperature profile starting at lower temperature with temperature increasing during the extraction of PEG. Consider author such solution for improving of debinding efficiency?

The presented dissertation thesis of Ing. Eva Hnátková represent valuable results with high level quality of interpretation. The objectives of the dissertation were fulfilled and the work meets the criteria for a doctoral study. Based on this, after a successful defence, I suggest Ing. Eva Hnátková to be awarded with the title

„philosophiae doctor“, PhD.

Bratislava, 15.5.2019                                       prof. Ing. Pavol Alexy, PhD.